Advanced Light Control Film-Polycarbonate (ALCF-P)

Description

ALCF-P Film is 3M’s latest version of LCF (Light Control Film), often referred to as louver film. Utilizing 3M’s proven and effective manufacturing technologies, ALCF-P film features a continuous matrix of black louvers embedded within the film. Primarily intended to limit viewing from off-axis positions for privacy reasons, it can also provide contrast enhancement and greater sunlight readability. It is also useful in redirecting light, such as eliminating nighttime reflections in automotive instrumentation and aerospace avionics applications. It is thinner than previous versions, yet keeps light loss to a minimum.

3M Innovation

Construction:

Illustrations are not necessarily drawn to scale, and all dimensions are nominal.

The film is available in several versions. Illustrated above is ALCF-P ABR2 and ABR0 Film. 
ALCF-P ABR2 film has an abrasion resistant matte hard coat on the top surface, and a glossy hard coat
on the bottom surface. ALCF-P ABR0 film has neither the top nor bottom hard coat layers.

Typical Configuration

The most common application is to mount the ALCF-P Film on the outside of the display underneath the touch screen if there is one. Certain touch screens will allow mounting underneath the ALCF-P film, and this feasibility should be determined by experimentation or by consulting your touch screen supplier. In addition, the ALCF-P film can sometimes be mounted inside the display behind the LC panel, although this will somewhat limit its ability to block off-axis images in privacy applications. Once again, experimentation should determine the efficacy of this configuration. See illustration on next page.

Laminating and Bonding

ALCF-P ABR0 film is recommended for applications where the film is laminated or bonded to another surface such as glass. To prevent scratching or damaging the ALCF-P ABR0 film, the protective liners should remain on the film during the fabrication or converting operations. Bonding techniques and specifications are the responsibility of the integrator.

In addition, ALCF-P film is usually mounted with the louvers running vertically, so as to limit the viewing angle from the sides (in the horizontal plane). However, applications involving contrast enhancement, sunlight readability, or reflection abatement, usually require limiting ambient light from above. In these cases, ALCF-P film would then be mounted with its louvers oriented horizontally.

ALCF-P Film above touch screen, or below touch screen, or below LC panel

Moiré Prevention:

Moiré is the shadowy appearance of stripes or lines, curved or straight that can occur in an LCD due to the optical interaction of regularly spaced elements within the display. The regularly spaced louvers of ALCF-P film may cause this optical interaction with the pixel grid of the LC panel, and thus result in moiré.  If encountered, moiré can be greatly reduced or entirely eliminated by converting the ALCF-P film at a slight bias offset angle. Experimentation has shown that an offset bias angle of 1 to 12 degrees will usually take care of the problem.

The direction of the louvers can be determined by looking closely at the film, where very fine, closely spaced streaks or lines can be noticed. These are the louvers. To help you determine the film orientation view the film off-axis from the side.

#### Formats: Reference the current price sheet or call your local sales rep or customer service (1-800-553-9215) for information on part sizes or request for custom part quotes.

General Converting, Assembly, and Handling Recommendations:

During converting operations, both the front and rear protective liners should remain on the film.

Die cutting is the recommended form of converting and will result in the cleanest edges, although shear cutting and laser cutting may also be acceptable. Whatever method used, you should ensure that the part has clean, crisp edges without any raggedness or other damage.

If installed behind the LC panel, the part should be precisely cut so as to provide a close fit in the cavity, yet not so close as to experience binding or warping problems from thermal expansion. Also, the part should be left free-floating in the cavity to avoid warping or buckling.  If necessary, the part may be tacked down along one edge or 2 adjacent corners with a double-coated optically clear tape, such as 3M MP468. Designs incorporating mounting tabs or holes mated to mounting pins are also popular.

Remove both protective liners by tacking near an edge or corner with a piece of aggressive tape and pulling gently.

Be aware that handling any polymer film can generate electrostatic charges that can attract dust and debris.

Remove any loose debris from the film by using compressed air.

Avoid fingerprints and debris by wearing clean latex gloves and holding the product at the edges.

Keep the area very clean to lessen the likelihood of debris contamination. Maintaining class 1000 clean room conditions is recommended.

Using anti-static measures, such as ionized air blowers whenever possible, is recommended.

As always, protect the film, especially the edges, from any undue shock or stress.

Storage

Material should be stored in its original packaging, laying in a horizontal orientation, away from direct sunlight.

Heavy objects should not be piled on top of it to avoid damaging the product. Ambient temperature and humidity should be controlled to 10–30 degrees C at 50 ± 20% R.H.

Important Notice to Purchaser

The following is made in lieu of all warranties, express or implied, including any implied warranties of

merchantability or ﬁtness for a particular purpose.

3M warrants that, at the time of shipment, product will meet 3M’s published specification or that specification

agreed in writing between 3M and purchaser, for twelve months after the date of receipt at purchaser’s location

provided that the product is stored flat in accordance with the requirements in the section titled Storage above and

in the original package. Should product not meet specifications at time of shipment and for twelve months

thereafter, 3M will replace or refund the purchase price of such quantity of the product found not to meet

specifications. Given the variety of factors that can affect the use and performance of a 3M Display Materials

& Systems Product (the “Product”), some of which are uniquely within the user’s knowledge and control, it is

essential that the user evaluate the 3M Display Materials & Systems Product to determine whether it is suitable for

user’s particular purpose and suitable for user’s method of application. 3M Display Materials & Systems’ statements,

engineering/technical information, and recommendations are provided for user’s convenience, but their accuracy or

completeness is not warranted.

3M shall not be liable under any legal theory, including in contract or in tort, for any injury, loss, or damage,

whether direct, indirect, incidental, special or consequential, arising out of the use of or the inability to use

the product.

The warranties and remedies set forth herein are purchaser’s sole and exclusive warranties and remedies.

Display Materials and Systems Division

3M Center, 235-1E-54

St. Paul, MN 55144-1000

www.3m.com/displayenhancement | 1-800-553-9215	Minimum 10% Post-Consumer Fiber

75-0500-5136-8

# Text boxes

3M is a trademark of 3M.

Scotch is a registered trademark of 3M.

Printed in U.S.A.

© 3M 2015. All rights reserved.

75-0500-5136-8   28577SA042715JF